## Slide 1: 辐照 vs 非辐照
李桃
2020/5/19

## Slide 2
Irradiated
Non-irradiated
Morphology
Morphology
Surface Potential
Surface roughness
Non-irradiated: 12.262 nm
Irradiated: 15.575 nm
Potential histogram
52mV
309mV
(Mean values after Gaussian fitting are labelled.)

## Slide 3
Potential histogram
Non-irradiated
Irradiated
(a)
(b)
(c)